## Slide 1: Pavement Materials Innovation with Recycled Tire Rubber & Balanced Mix Design

## Slide 2: NCAT Pavement Test Track
National Center for Asphalt Technology @ Auburn since 1986
Innovative, relevant, and implementable research projects
Advancement of safe and sustainable asphalt pavements
Mix/materials86, structural pavement design03, and preservation12
1.7-mile nonprofit Track since ‘00, rebuild/reset every 3 years.

## Slide 3: 11 States + FHWA + 8 Industry

## Slide 4: 2021 NCAT Pavement Test Track
32 sponsored sections
  16 traffic continuations
  7 mill/inlay sections
  9 structural sections
16 repaved/rebuilt sections
  ~1/3 of the Track (typical).

## Slide 5: Traffic Continuations16
Higher RAP with recycling agents – CAN3
Foamed cold central plant recycle (CCPR) base – VAN4
High performance thinlays (DGA, SMA) – ALN10,N11
Crack prevention interlayers – GAN12,N13
Soybean based polymer modified asphalt – SBW10
BMD via recycling agents, gradation change, etc. – OKS1, TXS10,S11
Impact of base stabilization, subgrade modification – MSS2
Long term benefit of surface rejuvenators – MSS3
Full depth rapid rebuilds (grinding vs thinlays, HiMA) – SCS9
Open graded friction surface rejuvenation – SRE1
Impact of density on performance – FLE5,E6

## Slide 6: 2012 “Green Group” Experiment
Purpose of Each Layer | N5 Control | S5 Higher RAP | S6 RAP+RAS | S13 Recyc Tires
Durable, Rut Resistant Surface | 20% RAP20 67-22/82-16 DG | 25% RAP11 67-22/76-22 SMA | 5% RAS21 67-22/88-16 SMA | VIRGIN 82-2212 SMA
Stiff, Strain Reducing Middle | 35% RAP39 67-22/88-10 DG | 50% RAP41 67-22/82-16 DG | 50% AGED26-24 67-22/94-10 DG | 35% RAP37 82-2212 DG
Fatigue Resistant Base Layer | 35% RAP39 67-22/88-10 DG | 35% RAP34 94-28/94-10 DG | 25% RAP24 +76-22/88-16 DG | VIRGIN 88-2220 AZ
Green = Evotherm Q1 Additive, Blue = Astec Green Foamer
“Coarse” RTR at ~17,000 pounds per mile of paving
13½ lbs
11½ lbs
29 lbs

## Slide 7: 2012 “Green Group” Experiment

## Slide 8: 2015 “Cracking Group” Experiment

## Slide 9: 2018 Reflective Crack Prevention Interlayers

## Slide 10: New Mill/Inlay Sections7
BMD via additives, gradation – OKN8,N9, TXN6
BMD with SGC and Marshall for QC – TNS4
Bond strength with different tack products and/or rates – NCW4
“BMD+Friction” mix optimization – KYS7
High performance OGFC surface – ALE9

## Slide 11: “Dry” Recycled Tire Rubber in N92021

## Slide 12: New Structural Sections9
Minimum HMA thickness over cold (re)recycling – VAS12
Additive Group (AG) study for additive impact on pavement life
“AG+” New polymer from old recycled tire rubber – Sigmabond HPS8
“AG+” High polymer performance with reduced viscosity – BASFS13

## Slide 13: 2021 Additive Group (AG) Study
Performance
Framework

## Slide 14: Phase 1 Studies (BMD+Fatigue)

## Slide 15: Balanced Mix Design for AG+ Study

## Slide 16: Fatigue Testing and Modeling

## Slide 17: Agency Selected AG Treatments
Recycled tire rubber
  “Dry” Smart Mix in PG67-22N1
  “Wet” Entech PG76-22N2
Recycled low density plastic
  “Dry” pellets with PG76-22S5
  “Wet” Dow with Elvaloy PG76-22S6
High strength aramid fibers
  Surface Tech ACE XP with PG76-22N5
Control with PG76-22N7
MnROAD in 2022

## Slide 18: Astec Double Barrel with Hi-Tech Feeder

## Slide 19: Hi-Tech Asphalt Solutions Feed System
 Smart Mix12
Dry Plastic8½
 Asphalt Plus12

## Slide 20: Smart Mix12
13½ lbs “fine” RTR per ton of asphalt
Great Lakes area source
Moving to GA for ‘22 AL projects
2M AL tires processed in GA
AL intake increase likely in ’22.

## Slide 21: Inline Vibrating Wire Viscometer
Neat Binder
SBS-Modified
“Wet” RTR

## Slide 22: Bulk Research Sampling

## Slide 23: Track Takeaways
Regional investigation/adoption of BMD requirements
Additives are nothing to fear by industry/agencies
Gap graded rubber mix in top, bottom, middle layers
BMD compliance is “easier” than volumetrics
“Easy Button” for dialing up IDEAL-CT?
Higher cracking indicator from production
No critical aging for non-surface mixes
No difficulty meeting densities with healthier mixes.

## Slide 24: Questions and Answers