## Slide 1: 3D Printing Soils using Bio-cementation Techniques
Michelle L. Barry, PhD, PE
Associate Professor, Civil Engineering
mlbernha@uark.edu
Christina Childress
Graduate Research Assistant

## Slide 2
Background
Additive Manufacturing or 3D Printing
FDM
SLA
SLS
PBBJ
EXTRUSION

## Slide 3
Background:
Microbially Induced Calcite Precipitation (MICP)
(1)
(2)
Notes: Most common method for activating calcite precipitation is Urease hydrolysis Eq. 1. Once carbonate ions precipitate the ions react with calcium to form calcite Eq. 2.

## Slide 4
Background:
SEM images of MICP

## Slide 5
Background:
MICP Methods
Injection method (pictured here).
Premixing method
Surface spraying method
(Konstantinou et al., 2021)

## Slide 6
Background: Injection method
Field-scale Application: Borehole Stabilization
(van Paassen, 2011)

## Slide 7
Background: Injection method
Field-scale Application: Scour Resistance
(Do et al., 2020)

## Slide 8
Background: Injection method
Field-scale Application: Liquefaction Resistance
(van Paassen et al., 2009)

## Slide 9
Background: Premixing method
Laboratory-scale Application: Additive Manufacturing
(Nething et al., 2020)

## Slide 10
Background: Spraying method
Field Scale Application: Coastal Erosion Resistance
(Kumar et al., 2020)

## Slide 11
Background: MICP
Alter soil classification
Increased Strength
Increased cohesion
Decreased compresibility
Decreased permeability
Increased friction angle
EFFECTS OF MICP ON ENGINEERING PROPERTIES

## Slide 12
MICP Spray Methodology
Sporosarcina Pasteurii Bacteria
Solution Preparation & Process
Urea-calcium solution (1.5:1)
Yeast extract
Ammonimum sulfate
Agar
Tris buffer
Scanning spectrophotometer at 600 nm wavelength
Electrical conductivity

## Slide 13
MICP Spray Methodology
Prototype Spray System & Process

## Slide 14
MICP Spray Methodology
Soil Mixtures Considered
50% Clay 50% Sand
100% Ottawa Sand

## Slide 15
Results: Depth and Spread
Determining the layer thickness and spread for each soil type
100% Ottawa Sand
0% Ottawa Sand
25% Ottawa Sand
50% Ottawa Sand
75% Ottawa Sand

## Slide 16
Results: Strength
50% Clay - 50% Sand Mixtures
 | Optical density | Spray volume (mL) | Density (g/cm3) | Peak stress (kPa)
Treated | 0.58 | 2.6 | 1.588 | 233.3
 | 0.58 | 2.6 | 1.594 | 262.6
 | 1.00 | 2.6 | 1.605 | 152.2
 | 1.00 | 2.6 | 1.583 | 220.1
Untreated | n/a | 2.6 | 1.627 | 162.9
 | n/a | 2.6 | 1.566 | 70.3

## Slide 17
Results: Strength
50% Clay - 50% Sand Mixtures
 | Optical density | Spray volume (mL) | Density (g/cm3) | Peak stress (kPa)
Treated | 0.58 | 2.6 | 1.588 | 233.3
 | 0.58 | 2.6 | 1.594 | 262.6
 | 1.00 | 2.6 | 1.605 | 152.2
 | 1.00 | 2.6 | 1.583 | 220.1
Untreated | n/a | 2.6 | 1.627 | 162.9
 | n/a | 2.6 | 1.566 | 70.3

## Slide 18
Future Applications
Cemented Soil Columns
Cemented Soil Geo Cells
Vertical construction

## Slide 19
Michelle L. Barry, PhD, PE
Associate Professor, Civil Engineering
mlbernha@uark.edu