## Slide 1: Why Do You Lose Air Volume When Pumping Air-Entrained Concrete??? and Why Does the Air Come Back?
Justin Becker, Nick Seader, Chad Staffileno
Tyler Ley PE, PhD

## Slide 2: Acknowledgements
Oklahoma DOT
FHWA
Colorado DOT
Kansas DOT
Nebraska DOT
Iowa DOT
Minnesota DOT
Idaho DOT
North Dakota DOT
Pennsylvania DOT
Connecticut DOT
Illinois DOT
Indiana DOT
Michigan DOT
Wisconsin DOT
New Jersey DOT
RMC Foundation
American Concrete Pumping Association

## Slide 3: Acknowledgements
Vermont DOT
Jim Wild
Justin LaRoche

## Slide 5: Overview
Why do we add air to concrete?
Why do pumps change the air content of concrete?
Why does the air come back?
If you see Pistol Pete then that means that something is very important!!!!

## Slide 6: Why Do We Add Air to Concrete?
Air-entrained bubbles are a key to the freeze-thaw resistance of concrete
Air volume = freeze-thaw performance
Smaller bubbles are more effective in providing freeze-thaw resistance and have less of an impact on our concrete than larger bubbles

## Slide 7
Volume of air provided is the same for both.
Case B has a better air void distribution.
A
B
What Do You Want in an Air-Void System?

## Slide 8
A
B
Volume of air provided is the same for both.
Case B has a better air void distribution.
What Do You Want in an Air-Void System?

## Slide 9: AASHTO R101
Freeze Thaw Field Acceptance
Super Air Meter
Air Volume > 4%
SAM Number < 0.30

## Slide 10: AASHTO R101
Freeze Thaw Field Acceptance
Super Air Meter
Air Volume > 4%
SAM Number < 0.30
Where is this from?

## Slide 11
What air content do you use?
3.5 Months
5 mins
Recommended
Not
Recommended

## Slide 12
What air content do you use?
Small bubbles
Large bubbles
3.5 Months
5 mins
Recommended
Not
Recommended

## Slide 13
Cliff of Doom
98 mixtures
91% agreement
Recommended
Not
Recommended
3.5 Months
10 mins

## Slide 14: UNC Charlotte

## Slide 15: Discussion
The SAM Number can better predict freeze thaw performance than the air volume.
The SAM Number can be determined in fresh concrete in about 10 mins.

## Slide 16: Why are we doing this?
Concrete pumps are essential tools in the industry but it is hard to predict how pumping will impact the air void system in concrete.

## Slide 18
Concrete is delivered here

## Slide 19
Concrete is delivered here
Concrete is sampled here

## Slide 21
Ready Mix
General Contractor

## Slide 22
Ready Mix
General Contractor
I brought you concrete with the right air!

## Slide 23
Ready Mix
General Contractor
I brought you concrete with the right air!
It doesn’t have the right air any more!!!

## Slide 24: How do people deal with this?
Increase the air volume before it goes into the pump so that it still has enough air when it comes out.
One time this worked….

## Slide 25: Mechanisms
1. Pressure
2. Vacuum
3. Impact
How does pumping change air?

## Slide 26: Mechanisms
1. Pressure
2. Vacuum
3. Impact
How does pumping change air?

## Slide 27: Methods
Investigate the following before and after pumping:
Air volume
SAM Number (air void spacing) AASHTO T 395
Spacing factor (air void spacing) ASTM C 457
Freeze-thaw performance ASTM C 666

## Slide 28: Mixture Design
0.45 w/cm
20% Class C ash
6.5 sacks (611 lbs)
Limestone and natural sand
5” to 8” slump
Air contents from 4% to 8%
With and without water reducer/retarder
33 lab mixtures

## Slide 30: Pipe Network

## Slide 31: Lab Pumping Information
4” diameter pipe
60’ of steel pipe
10’ Rubber hose
pumping pressures from 55 to 110 psi

## Slide 32
Lab data

## Slide 33
Lab data
Pumped concrete
Non-pumped concrete

## Slide 34: Summary
33
Fresh Air > 4.0%
SAM # < 0.32
Before Pumping
After Pumping
Hardened Concrete
Notes: Acceptable before pumping, Air greater than 4% and SAM less than 0.30.

## Slide 35: Summary
33
Fresh Air > 4.0%
SAM # < 0.32
11
Fresh Air > 4.0%
SAM # < 0.32
Before Pumping
After Pumping
Hardened Concrete
22
Fresh Air < 4.0%
SAM # > 0.32
Notes: Acceptable before pumping, Air greater than 4% and SAM less than 0.30.

## Slide 36: Summary
33
Fresh Air > 4.0%
SAM # < 0.32
11
Fresh Air > 4.0%
SAM # < 0.32
33
ASTM C666
Durability Factor > 70%
Before Pumping
After Pumping
Hardened Concrete
22
Fresh Air < 4.0%
SAM # > 0.32
Notes: Acceptable before pumping, Air greater than 4% and SAM less than 0.30.

## Slide 37
A Clue!!!
Fresh air content after pumping
Hardened air content after pumping
Notes: Acceptable before pumping, Air greater than 4% and SAM less than 0.30.

## Slide 38
Hardened air higher than fresh air
Hardened air lower
than fresh air

## Slide 39
Variation of test method
Line of agreement

## Slide 40: Discussion
Satisfactory freeze thaw performance of pumped concrete was observed even though there were low air contents and high SAM Numbers after pumping.
BUT! There is minimal change in the spacing factor measured on the hardened concrete taken before and after pumping.

## Slide 41: Discussion
The hardened and fresh measurements closely matched prior to pumping.
After pumping the hardened air content was on average 1.15x higher in the fresh air content.
For example – After pumping 6% fresh and about 7% in hardened concrete
The fresh measurements after pumping do not represent the performance or properties of the hardened concrete.

## Slide 42: Reliable
33
Fresh Air > 4.0%
SAM # < 0.32
11
Fresh Air > 4.0%
SAM # < 0.32
33
ASTM C666
Durability Factor > 70%
Before Pumping
After Pumping
Hardened Concrete
22
Reliable
Unreliable
Fresh Air < 4.0%
SAM # > 0.32
Notes: Acceptable before pumping, Air greater than 4% and SAM less than 0.30.

## Slide 43: Does this hold for other equipment and mixtures? What is going on in the field?

## Slide 44: Field Pumping Information
30 different projects
62 different mixtures tested
Bridge decks, walls, sidewalk, parking lot, drilled shaft
18 Different Types of Pumps
Boom lengths ranged from 100’ to 180’
Pipes from 4” to 6” in diameter
Used three different boom configurations

## Slide 45
Flat
Arch
A-Frame

## Slide 46: Pump configurations
Flat
Arch
A-frame

## Slide 48
24% Decrease
- 35% A-Frame
- 21% Arch

## Slide 49
0.098 offset

## Slide 50
29% Increase
- 32% A-Frame
- 44% Arch
- 40% Flat
0.098 offset

## Slide 51: Discussion
Air Content
  24% of samples show a significant decrease
  A-frame caused the most impact on the air volume after pumping
SAM Number
  29% of samples increased significantly
  Arch configuration caused the most impact on void spacing after pumping

## Slide 52: How about the hardened concrete?

## Slide 54
23% Increase!

## Slide 55
Arch results are similar. Flat shows little loss in air.
55
Hardened air higher than fresh air
Hardened air lower
than fresh air
After Pumping
Before Pumping
Field data

## Slide 57: Discussion
The hardened and fresh measurements closely matched prior to pumping.
After pumping the hardened air content was on average 1.15x higher than the fresh air content.
For example – After pumping 6% fresh and about 7% in hardened concrete
There is no significant change in the spacing factor when comparing data before and after pumping.

## Slide 58: Discussion
These are the same findings from the lab but with different pump configurations, equipment, and materials!!!!
The fresh measurements after pumping do not seem to represent the performance or properties of the hardened concrete.

## Slide 59: What is happening?

## Slide 60: What is happening?
Back to the lab!!!!

## Slide 61: Where does the air change within the pump network?

## Slide 62
a
b
c
d
e
f

## Slide 63
Chart: Feet along pipeline
| 0 | 3.3 | 6.6 | 19.7 | 25.4 | 34.299999999999997 | 44.1
 | 0.08 | 0.051 | 0.048 | 0.047 | 0.05 | 0.051 | 0.051
 | 0.086 | 0.059 | 0.062 | 0.063 | 0.065

## Slide 64: Discussion
The air is lost right after the pump and stays almost constant throughout the pipe network.
Additional piston strokes (pressure cycles) did not cause additional air to be lost.
The air loss coincides with point of highest pressure.

## Slide 65: Why does this happen?
  Henry’s Law – p=kc
      p=partial pressure of the gas
      c=concentration of the dissolved gas in solution
      k=constant
  Pressure
  Dissolved gas

## Slide 66: Air and SAM over time
We pumped concrete and measured how the air volume and SAM Number change over time.
15 min
30 min
45 min
Sampling time
after pumping

## Slide 69
Bubbles go away
Bubbles come back?

## Slide 72
Bubble spacing increases
Bubble spacing decreases?

## Slide 73: What is happening???
The pressures from pumping causes the small bubbles to temporarily dissolve
But good performance in the petrographic analysis, freeze-thaw testing, and reducing SAM Number over time suggests that the dissolved air comes back before the concrete hardens.
When the air comes back it seems to be well dispersed and provides a similar spacing factor to what went into the pump.

## Slide 74
Notes: Acceptable before pumping, Air greater than 4% and SAM less than 0.30.

## Slide 77
BUBBLES

## Slide 78: What does this mean?
Air Content and SAM testing after pumping are not representative of the hardened concrete.
If this is true then concrete should not be rejected for low air or high SAM Number after pumping.
It appears that sampling the concrete prior to pumping is a good indicator to the air void system in the hardened concrete.

## Slide 79: What do I think needs to happen?
Testing air at the point of discharge from a pump is dangerous and it is not representative of the properties of the hardened concrete.
We need to test concrete before pumping and not require testing at the point of placement.

## Slide 81
Concrete is delivered here

## Slide 82
Concrete is delivered here
Concrete is sampled here

## Slide 83: What do I think needs to happen?
I think our air testing needs to be done with the SAM because it better correlates with freeze thaw performance.
We need to have local discussions about how we need to change specifications and construction practices.

## Slide 84
OK
Doing research
MN, IA, WI, KS, AR

## Slide 85
OK
Doing research
MN, IA, WI, KS, AR
12 States no longer test before the pump

## Slide 86: Specification changes are being discussed in the following states
Minnesota
Iowa
Wisconsin
Kansas
Arkansas

## Slide 87: Specification changes
FHWA is sponsoring more research with me right now to produce more data.
The testing is done and we are preparing the reports.
There are no changes to my conclusions or recommendations.

## Slide 88: Conclusion
Pumping was observed to modify the air content and SAM Number in both the lab and the field testing.
Based on the hardened air void analysis, freeze thaw testing, and changing SAM Number over time, the small bubbles seem to return to the concrete with a similar air void distribution and freeze thaw performance as was in the concrete before pumping.
The SAM was an invaluable tool to give insights into the performance of air before and after a concrete pump.

## Slide 89
www.youtube.com/tylerley

## Slide 90
Questions?
www.tylerley.com
Tyler.ley@okstate.edu

## Slide 92: What can I do to avoid air loss?
Air loss seems to happen more in the following situations:
  Higher pumping pressures
  Smaller diameter lines
  Mixtures with poor aggregate gradations
  Lower slump mixtures
  A-frame and arch configurations

## Slide 93: How does this change the bubble size distribution?

## Slide 94
2”
2”
0.75”
0.75”

## Slide 96
Air pump

## Slide 97
pressure step 0
atmospheric pressure
synthetic AEA

## Slide 98
pressure step 1

## Slide 99
pressure step 2

## Slide 100
pressure step 3

## Slide 101
pressure step 4

## Slide 102
pressure step 5

## Slide 103
pressure step 6

## Slide 104
pressure step 7

## Slide 105
Atmospheric pressure

## Slide 106
pressure step 0
atmospheric pressure

## Slide 107: Discussion
1. As the pressure increases the small bubbles dissolve into the surrounding solution
2. These bubbles do not immediately come back when you decrease the pressure.

## Slide 108: Why do the small bubbles dissolve???
  Laplace-Young Equation
  P1=P0+4σ/d
        P1=internal pressure of the air bubble
        P0=pressure of fluid surrounding the bubble
        σ=surface tension of the bubble film
        d=bubble radius
This means the small bubbles have higher pressure than the large bubbles.

## Slide 109: Why do the bubbles dissolve?
The small bubbles have a large curvature. This makes it easier for the bubble walls to become damaged and the air will dissolve.
Why do the small bubbles dissolve???

## Slide 111: What does this mean?
The pressures during pumping causes the small bubbles to dissolve and so they are not present in the fresh concrete when it discharges from the pump.
This is why the air volume decreases and the SAM Number increases.

## Slide 112: Remember!!!!

## Slide 113: Remember!!!!
This means the air comes back with about the same spacing

## Slide 114: What does this mean?
Air Content and SAM testing after pumping are not representative of the hardened concrete.
If this is true then concrete should not be rejected for low air or high SAM Number after pumping.
It appears that sampling the concrete prior to pumping is a good indicator to the air void system in the hardened concrete.

## Slide 115: What do I think needs to happen?
Testing air at the point of discharge from a pump is dangerous and it is not representative of the properties of the hardened concrete.
We need to test concrete before pumping and not require testing at the point of placement.

## Slide 116: What do I think needs to happen?
I think our air testing needs to be done with the SAM because it better correlates with freeze thaw performance.
We need to have local discussions about how we need to change specifications and construction practices.

## Slide 118
Concrete is delivered here

## Slide 119
Concrete is delivered here
Concrete is sampled here

## Slide 120
Ready Mix
General Contractor
I brought you concrete with the right air!

## Slide 121
Ready Mix
General Contractor
I brought you concrete with the right air!
YAY!!!
I love you.

## Slide 122
BUBBLES

## Slide 123: Conclusion
Pumping was observed to modify the air content and SAM Number in both the lab and the field testing.
Based on the hardened air void analysis, freeze thaw testing, and changing SAM Number over time, the small bubbles seem to return to the concrete with a similar air void distribution and freeze thaw performance as was in the concrete before pumping.
The SAM was an invaluable tool to give insights into the performance of air before and after a concrete pump.

## Slide 124: Quick update on spec changes
Alaska, New York, Oklahoma, Utah and Oregon do not test after the pump in most conditions.
Minnesota, Wisconsin, Kansas, and Arkansas are doing their own testing to change their specs.
FHWA is sponsoring more research with me right now to produce more data. The testing is done and there are not changes in my conclusions.

## Slide 125
www.youtube.com/tylerley

## Slide 126
Questions?
www.tylerley.com
Tyler.ley@okstate.edu

## Slide 128
BUBBLES

## Slide 129: Sam Field Study
21 State DOTs + 1 Canadian Province helped analyze 231 concrete mixtures from 110 different projects
More than: 15 different SAMs and operators, 62 different aggregates, 19 cement sources, 20 different fly ashes , 39 different admixtures
60% pavements, 20% bridge decks, and 20% other
self-consolidating, precast, ready mix, and central mix concrete
Thank you to all that helped!

## Slide 130: What air content do you specify?
0.008”
spacing factor
Air content between 3.75% and 7.75% for 0.008” spacing factor
231 field mixes

## Slide 131
0.008”
spacing factor
Air content between 3.75% and 7.75% for 0.008” spacing factor
231 field mixes
These mixtures have good air contents and spacing factors that are not recommended
BAD BOX!

## Slide 132
0.008”
spacing factor
Air content between 3.75% and 7.75% for 0.008” spacing factor
231 field mixes
These mixtures have good air contents and spacing factors that are not recommended
BAD BOX!
1/4 have a spacing factor > 0.008”

## Slide 133: Summary
We need to know the size of bubbles within the concrete
The volume of air does not tell you about bubble size
25% of the time we are accepting concrete that does not meet the recommended air void quality
What if we could measure this in the fresh concrete???

## Slide 134: Other studies with similar findings
Iowa DOT
Pennsylvania DOT
Vermont DOT
NCHRP Project lead by Peter Taylor
Lafarge Holcim
UNC Charlotte
Polish Researchers

## Slide 135: Limits to signify a significant change
In order to determine if the air volume and spacing factor significantly changed the following standard deviations and coefficient of variations were used.
Concrete Parameter | 95% Confidence Boundary (2SD’s) | Referenced Standard
Fresh Air Content (%) | 0.7 | ASTM C231
SAM Number | 0.098 | AASHTO TP 118
Hardened Air Content (%) | 1.42 | ASTM C457
Spacing Factor (%) | 40.2* | ASTM C457

## Slide 136
Hardened Air Void Analysis
From Hover

## Slide 137
Hardened Air Void Analysis
From Hover

## Slide 138
Freeman et al., 2012
small voids
large voids
frequency

## Slide 139
Freeman et al., 2012
small voids
large voids
frequency
Small bubbles
Large bubbles

## Slide 140
Spacing Factor – ½ of the average distance of an average sized void uniformly distributed in the paste
Desired Value < 0.008 in (ACI 201)
real concrete
idealized concrete
Spacing factor
from Hover

## Slide 141
Freeman et al., 2012
small voids
large voids
frequency
Low spacing factor
High spacing factor

## Slide 142
Ley et al., 2017
Small Bubbles
Large Bubbles

## Slide 143: Summary
We need to know the size of bubbles within the concrete
The volume of air does not tell you about bubble size
What if we could measure this in the fresh concrete???

## Slide 144
digital
gauge
six clamps!
Super Air Meter
(SAM)

## Slide 145
Ley et al., 2017
Small Bubbles
Large Bubbles

## Slide 146
Ley et al., 2017
Small Bubbles
Large Bubbles

## Slide 147
Over 227 lab mixtures from two different research groups
Ley et al., 2017
0.008”
spacing factor
10 mins in fresh concrete
14 days
88% agreement

## Slide 148
What about freeze thaw?

## Slide 149
Lab data

## Slide 150
Lab data
Pumped concrete
Non-pumped concrete

## Slide 151
Small Bubbles
Large Bubbles