## Slide 1: Using BCSA Cement for Structural Concrete
Cameron Murray, Ph.D., P.E., Assistant Professor, University of Arkansas
Gabe Johnson, Elizabeth Poblete, Behzad Farivar, GRA, U of A
Gabe Cook, Oncor Electric Delivery, Ft. Worth, TX
Edgar Soriano, WSP, Indianapolis, IN
Gerardo Aguilar, Construir Futuro, Quito, Ecuador
Caleb Chesnut, Martin/Martin, Bentonville, AR

## Slide 2: BCSA Cement in Structural Concrete

## Slide 3: BCSA Cement in Structural Concrete
BCSA cement’s properties are useful for precast/prestressed and structural repair
  Low shrinkage
  Fast setting/fast strength gain
  Many practical questions remain
Past work at University of Oklahoma on prestressed concrete
  Improved prestress losses
  Good flexural strengths
  Good bond to prestressing strands

## Slide 4: Initial Practical Concerns
globalgilson.com
Slump and Water Content
Setting Time of BCSA Cement
100 F Ambient Temp. Example

## Slide 5: Initial Practical Concerns
w/c – strength relationship similar to PC
  3 hour strength
  28 day strength

## Slide 6: Flexural Strengths of BCSA Cement Concrete
12 reinforced concrete beams made with either PC or BCSA cement
  6 Tension Controlled
  6 Compression Controlled
Tested at different ages
Cook, G.W., Murray, C.D., “Early Age Performance of Reinforced Concrete Beams Made with BCSA Cement.” ACI Materials Journal 117, no. 01 (2020).

## Slide 7: Flexural Strengths of BCSA Cement Concrete

## Slide 8: Flexural Strengths of BCSA Cement Concrete

## Slide 9: Flexural Strengths of BCSA Cement Concrete

## Slide 10: Flexural Strengths of BCSA Cement Concrete
BCSA Multi Hour
BCSA 1 Day
Weaker Concrete

## Slide 11: Current ACI CRC Study
Flexural stress-strain of BCSA cement concrete
Mertol, H. C., Rizkalla, S., Zia, P., and Mirmiran, A.” Characteristics of compressive stress distribution in high-strength concrete.” ACI Structural Journal, Vol. 105, No. 5. 2008.
εcu = 0.003
Strain
Stress

## Slide 12: Current ACI CRC Study
Mertol, H. C., Rizkalla, S., Zia, P., and Mirmiran, A.” Characteristics of compressive stress distribution in high-strength concrete.” ACI Structural Journal, Vol. 105, No. 5. 2008.

## Slide 13: Current ACI CRC Study

## Slide 14: Current ACI CRC Study

## Slide 15: Shear Strength of BCSA Cement Concrete
Chesnut, C.W. and Murray, C.D. “Shear Capacity of Reinforced Concrete made with BCSA Cement.” ACI Structural Journal 120, no. 1 (2023).

## Slide 16: Shear Strength of BCSA Cement Concrete
BCSA
PC

## Slide 17: Shear Strength of BCSA Cement Concrete

## Slide 18: Conclusions
Code procedures appear to be adequate for predicting BCSA concrete structural strengths
  True for flexural and shear strengths
Ongoing work investigating stress-strain relationships
Unique mixture design considerations
  But major benefit is similarities to PC

## Slide 19: Questions?
cdmurray@uark.edu
This material is based upon work supported by the Engineering Research and Development Center Geotechnical and Structures Laboratory (ERDC-GSL) under Contract No. W912HZ21C0037.