## Slide 1: MCTC and Emerging Concrete Technology
Robert Conway, PE CCM
Senior Pavement & Material Engineer
FHWA, Resource Center
2023 TRC Transportation Engineering Conference
May 24th 2023

## Slide 2: Mobile Concrete Technology Center
Funded by the Accelerated Implementation and Deployment of Pavement Technologies Program
Unique
Program evolves to meet stakeholder needs

## Slide 3: MCTC Team
Mike Praul
Jagan Gudimettla
Jim Grove
Nicolai Morari
Jerry Clemons
Josh Brinegar
Bob Conway
Lisa McDaniel

## Slide 4: MCTC Program Mission
Implement new & under-used concrete technologies
Demonstrate benefits of performance specifications in both agency quality assurance (QA) programs & industry quality control (QC) applications
Advance States’ concrete programs
  Specification review
  Technical assistance
  Training
  Troubleshooting
Better concrete

## Slide 5: Program Activities
Field visits to active construction projects
Quality in the Concrete Paving Process workshops
Equipment Loan Program
Technical assistance/specification reviews
Conferences/Open houses
Support TFHRC and other research
Publications to promote the FHWA concrete program and advance concrete technology

## Slide 6: MCTC Field Visits (since 2008)
WA
NV
MO
KS
IN
GA
NC
CA
WI
MN
IA
MI
PA
VA
CO
OR
AZ
AL
AR
NM
TX
OK
UT
FL
ID
WY
ND
NE
SD
IL
KY
WV
MD
DE
NJ
RI
VT
NH
ME
NY
OH
MT
MS
TN
LA
AK
SC
HI

## Slide 7: “Live From the MCTC” Training/Workshops
Super Air Meter (SAM)
Surface/Bulk Resistivity
Maturity
Box Test/V-Kelly
Semi-adiabatic calorimeter
Phoenix (fresh water content)
Pulse Induction Technology (MIT-SCAN-T3)
MIT-DOWEL-SCAN
HIPERPAV®
Optimized Gradation software

## Slide 8: MCTC Virtual Sessions (2020-2021)

## Slide 9: One Pager Series
New effort to use MCTC data
Narrowly focused
Meant to stir interest and point reader to resources
    1st: Cement content
    2nd: Optimized Mix Design
    3rd: Cores vs. Cylinders
    4th: NDT Pavement Thickness
    5th: Tining/Surface Texture
    6th: Surface Resistivity Test
    7th: Maturity
www.fhwa.dot.gov/pavement/concrete/trailer/resources
    8th: Curing
    9th: SCM’s
    10th: Calorimetry
    11th: Workability
    12th: Air Entrainment
    13th: Stringless Paving
    14th: Water Reducing Admixtures

## Slide 10: Technology Tour Across Ohio – 2 weeks, 6 cities

## Slide 11: MCTC Website
https://www.fhwa.dot.gov/MCTC

## Slide 12: 1. Optimized Gradation

## Slide 13: Performance Engineered Mixtures and Sustainability
Performance-type specifications; eliminate mandatory minimum cement content requirements
Optimize aggregate gradation
Use supplementary cementitious materials
Use maturity to determine opening times
Quality control during production to provide more consistent concrete
Ways to Optimize Cement Content

## Slide 14: Optimized Combined Gradation
What will it do for me?
  _____
  _____
  _____
  _____
  _____
  Less paste=> Lower permeability
  Less paste=> Reduced thermal shrinkage
  Less paste=> Reduced drying shrinkage
  Improved workability
  Reduce segregation potential
  Reduce cost
  Equal or higher strength
  Improve sustainability

## Slide 15: Achieving Optimized Combined Gradation
Existing analysis tools
  Shilstone Coarseness/Workability Factor Chart
  0.45 Power Chart
  Percent Retained on Each Sieve Chart (8-18 band)
Each tool tells us something different about the gradation
New analysis method – Tarantula Curve

## Slide 16: Optimized Gradation Tool
Spreadsheets available for structural or paving applications.

## Slide 17: Optimized?

## Slide 18: 2. Slump

## Slide 19: Changes in Slump Testing
  100 Years ago
  Today
What has changed?

## Slide 20: What do we really want to find out using the slump test?
Water content?
  Historically, an indicator of water content
  Today, water reducers will change the slump with no changed in water
  SCMs impact
Workability/flowability?
  Slump does not account for energy being added through vibration
Change
  Slump can ONLY tell us something has changed
  QC tool only
1922
Image Pixabay

## Slide 21: Box Test and VKelly

## Slide 22: Phoenix vs. Microwave Water Content

## Slide 23: 3. 56-day Testing

## Slide 24: MCTC Data

## Slide 25: Concrete Acceptance Practices
How do we accept concrete?
  Slump
  Strength
  Total air
  Temperature
  Thickness
  Ride
How do we adjust price?
  Strength
Lower Right Image: Pixabay

## Slide 26: The Great 28
Wrong time
Wrong cementitious system
Implications
  Cost
  Durability
  Deck Cracking

## Slide 27: 4. Resistivity Test

## Slide 28: Permeability
The ease with which fluids can penetrate the concrete
Only the paste contributes
Durability damage is governed by permeability
Amount of Pores (porosity)
How pores are connected (tortuosity)
Notes: Two biggest factors impacting durability are the amount of pores

## Slide 29: Resistivity Tests

## Slide 30: Resistivity Results
Curing of the cylinders is extremely important for SR
Consistent test procedure is necessary for comparison of results

## Slide 31: 56 Day Testing—A Real Example
Real Time QC
Heat Signature – Info in a day
Unit Weight – Real Time
Surface Resistivity at 56 Days
Acceptance
Surface Resistivity at 28 Days
Real time tests predict later age properties

## Slide 32: 5. Performance Specification/PEM

## Slide 33: Prescriptive vs. Performance Specifications
Agency dictates how the material or product is formulated and constructed
Based on past experience
Minimal/uncertain ability to innovate
Requires agency to have proper manpower and skill set to provide oversight
Prescriptive
Agency identifies desired characteristics of the material or product
Contractor controls how to provide those characteristics
Maximum ability to innovate
Reduced oversight burden on agency
Performance

## Slide 34: Performance Engineered Mixture Concepts
Get beyond slump, strength, and total air content as determinants of concrete quality
Incorporate tests that correlate to service life durability
Appropriately apply those tests in agency acceptance and contractor quality control programs
Develop specifications and practices to leverage quality control
Remove prescriptive restraints from specifications
  Minimum cement content
  Single aggregate gradation
  Slump

## Slide 35: PEM Pooled Fund and Incentive Projects
19 States + FHWA + Industry (December 2022)
PEM Implementation Incentive Pilot Projects

## Slide 36: Questions?
Image Pixabay
Contact info:
Robert.conway@dot.gov
202-906-0536