## Slide 13
“SOMEBODY NEEDS TO DO SOMETHING ABOUT THIS”
Notes: Work, school, church, aunt Lo Lou’s house- Late last summer the Materials Division started to float the idea that we want the people to take on anything falling into this category that is even remotely materials related.

## Slide 14
“SOMEBODY NEEDS TO DO SOMETHING ABOUT THIS”
Notes: The overwhelming and immediate response we got was Asphalt! Doesn’t Last, Isn’t durable, Cracks, too dry It needs more oil

## Slide 17
ADD MORE OIL

## Slide 19
SUPERPAVE ASPHALT DESIGN
Notes: The basic idea for a superpave design is for the ratio of these elements or (volumetrics) to be within the specified ranges at a specified compactive effort.

## Slide 20
Ninitial
Ndesign
Air Voids = 4.0%
VMA = 14.0 – 16.0
SUPERPAVE ASPHALT DESIGN
%Gmm @ Ninitial
VMA
Air
Voids
Notes: Graphic of Gyratory Compaction Ccuve

## Slide 21
Ninitial
Ndesign
ADD MORE OIL
VMA
Air
Voids
Notes: If we simply add more oli- likely hit target for volumetrics

## Slide 22
Ninitial
Ndesign
ADD MORE OIL
Air Voids @ Ndesign = lower
VMA @ Ndesign = higher
Rut depth = higher

## Slide 23
Ninitial
Ndesign
ADD MORE OIL
%Gmm @ Ninitial = higher
Notes: Side Note-You may see some jobs coming up where we recommend removing the Ninitial req. because mixes that are too sensitive should fail the rut test.

## Slide 24: TRC 2201: Update to ARDOT Superpave Gyratory Compaction Specification to Increase Pavement Durability
Notes: Chris Abade

## Slide 25
Notes: There are a lot of people
Lots of hands on the steering wheel
TRC 2201 will be the most successful

## Slide 26
Notes: There are a lot of people
Lots of hands on the steering wheel
TRC 2201 will be the most successful

## Slide 27
Notes: Stake holders -

## Slide 28
Notes: Meeting last fall
Shake Hands – Smile , but we are talking about change and there’s a little tension and some trust issues

## Slide 29
THE KEY TO SUCCESS

## Slide 30
Notes: Industry and even U of A buy it

## Slide 31
PRODUCE
AMAZING
ASPHALT
Notes: Not good, better, cheap
What does amazing asphalt look like?

## Slide 32
2015
2020

## Slide 33
2015
1998

## Slide 34
2015

## Slide 35
2015
1998

## Slide 36
1998

## Slide 37
1998
“SOMEBODY NEEDS TO DO SOMETHING ABOUT THIS”

## Slide 38
2020
Notes: How do we produce amazing asphalt??? I think all decisions related to asphalt need to be judged by this complex matrix

## Slide 41
RECYCLED ASPHALT PAVEMENT
Notes: DMS’s did a survey of every RAP stockpile in the state.

## Slide 44
Power BI Desktop
Distance 21
Signs 6
Method of Marking/Separating Stockpiles
Distance & Signs 2
0.0
0.5
1.0
Plant
Percent of RAP
APAC - Old Cas…
APAC Central - …
APAC Central - …
APAC Central - …
APAC TN - Forr…
APAC TN - Wes…
Atlas Asphalt - …
Atlas Asphalt - …
Atlas Asphalt - …
Blackstone - #1…
Cranford - Littl…
Delta Asphalt - …
Delta Asphalt - …
Delta Asphalt - …
Delta Asphalt - …
Diamond B Co…
Grant Garret Ex…
Hutchens Cons…
Hutchens Cons…
Hutchens Cons…
Jay-Pac - Plum…
North Central …
PBSG - #1 - Pin…
PBSG - #3 - Mo…
Redstone - #1, …
Redstone - Gur…
RK Hall - Texark…
Rogers Group -…
Rogers Group -…
RAP Sources
State Millings
Public Millings
Parking Lots
Plant Waste
Method of Processing RAP
Crush All 12
Screen & Crush Oversize 14
Screen Oversize 3

## Slide 45
Power BI Desktop
Frequency of Binder Content Testing
2000 tons 5
500 tons 5
Mix Design Only 5
1000 tons 3
As Required 2
Monthly 2
1500 tons 1
Biweekly 1
750 tons 1
250 tons 1
Weekly 1
Daily 1
Per Job 1
Method For Determination of Binder Content
Ignition Oven 26
Vacuum Extraction 3
Frequency of Gradation Testing
2000 tons 5
500 tons 5
Mix Design Only 5
1000 tons 3
As Required 2
Monthly 2
Daily 1
Biweekly 1
750 tons 1
250 tons 1
1500 tons 1
Weekly 1
Per Job 1
N/A 8
Mix Design Only 7
Yearly 5
500 Tons 4
1500 tons 1
Quarterly 2
1
Frequency of Specific Gravity Testing
Daily
Notes: Inconsisetncy with Quality Control Uniform acccross the industry-

## Slide 46
Notes: Quality Pavement Conference learning how to partner with the contractor
RAP Best Practices Specification

## Slide 47
Notes: When they saw things from our perspective – their attituedes

## Slide 49
Notes: More functional- Safer- Tied to Plant inspection
Reasonable Compliance
Go into effect in the November letting-Will soon be published on the PM website

## Slide 50: TRC 2201: Balanced Mix Design
Notes: Cross County

## Slide 54
Notes: Best possible resistance to Rutting and Cracking

## Slide 55
Chart: Performance Tests by Binder Contents
| 0.06 | 0.06 | 0.06
APA Limit (Upper) | 0 | 5 | 10
APA | 0 | 0.5 | 0.75 | 1 | 2 | 3 | 4 | 5 | 6 | 7
IDEAL-CT Limit (Lower) | 0 | 50 | 150
IDEAL-CT | 25 | 30 | 45 | 50 | 55 | 62 | 70 | 85 | 120 | 150

## Slide 56
Chart: Performance Tests by Binder Contents
| 0.06 | 0.06 | 0.06
APA Limit (Upper) | 0 | 5 | 10
APA | 0 | 0.5 | 0.75 | 1 | 2 | 3 | 4 | 5 | 6 | 7
IDEAL-CT Limit (Lower) | 0 | 50 | 150
IDEAL-CT | 25 | 30 | 45 | 50 | 55 | 62 | 70 | 85 | 120 | 150

## Slide 57
Chart: Performance Tests by Binder Contents
| 0.06 | 0.06 | 0.06
APA Limit (Upper) | 0 | 5 | 10
APA | 0 | 0.5 | 0.75 | 1 | 2 | 3 | 4 | 5 | 6 | 7
IDEAL-CT Limit (Lower) | 0 | 50 | 150
IDEAL-CT | 25 | 30 | 45 | 50 | 55 | 62 | 70 | 85 | 120 | 150

## Slide 58
Chart: Performance Tests by Binder Contents
| 0.06 | 0.06 | 0.06
APA Limit (Upper) | 0 | 5 | 10
APA | 0 | 0.5 | 0.75 | 1 | 2 | 3 | 4 | 5 | 6 | 7
IDEAL-CT Limit (Lower) | 0 | 50 | 150
IDEAL-CT | 25 | 30 | 45 | 50 | 55 | 62 | 70 | 85 | 120 | 150
VMA
Air
Voids

## Slide 59
Ninitial
Ndesign
VMA
Air
Voids
Notes: If we simply add more oli- likely hit target for volumetrics

## Slide 60
Ninitial
Ndesign
VMA
Air
Voids
Notes: If we simply add more oli- likely hit target for volumetrics

## Slide 62
Notes: Very intelligent kids that don’t really know anything about anything. Goals – Success- achievements like those are things you get to one day- and then your there. That mindset is why superpave design has reached the end of its useful life. Revising specifications, keeping up with performance, and addressing issues little by little is tedious, but if we do those things, and we continue seek improvement 15-20-25 years from now people will look at our pavements and be impressed- Unless they come from Texas